Copper Strand Thermal Shielding
for Third-Scale Magnet
Aritra Biswas
July 13, 2015 – nEDM Collaboration Meeting

---
Third-Scale Magnet
- superconducting lead
  (Tc = 7.2 K) for B field uniformity
- thermally-shielded warm bore to map B field
- copper plating on G-10 for insulation
- can't interfere with B field
thermal shield cover
warm bore

---
Our Thermal Shield

---
Our Thermal Shield
- strands of copper held together by epoxy
- currents can't jump between insulated strands
- no large-scale eddy currents
- measure B field effect and compare with copper plate

---
setup inside B0 coil driven by AC
alternating field in x direction
z
x
central axis
gain:
phase shift:
B_x
probe
B_x = B_0 \cos(\omega t + \psi)
B_x
probe
B_x' = B_0' \cos(\omega t + \psi')
\gamma \equiv {B_0' \over B_0}
\Delta\psi \equiv \psi' - \psi

---
Predicting γ(ω) and Δψ(ω)
induction on plate
x
B_{x,\mathrm{applied}} = B_0 \cos(\omega t + \psi)
\gamma = \sqrt{\alpha^2 + 1}
\Delta\psi = -\arctan(-\alpha)
I_i = {\mathcal E_i \over R_i} \sim \pd{}{t}[B_{x,\mathrm{applied}}]
B_{x,\mathrm{induced}} \sim \pd{B_{x,\mathrm{a}}}{t} = \alpha B_0 \sin(\omega t + \psi)
\textcolor{green}{I_i}
\begin{align*} B_{x,\mathrm{meas}} &= B_{x,\mathrm{appl}} + B_{x,\mathrm{ind}} \\ &= \gamma B_0 \cos(\omega t + \psi + \Delta\psi) \end{align*}

---
$0.04^{\circ} \pm 0.31^{\circ}$ deviation from 0

---
$(8.4 \pm 19.8) \times 10^{-4}$ deviation from $1$

---
Predicting γ(ω) and Δψ(ω)
skin depth attenuation
induction on plate
x
x
B_{x,\mathrm{applied}} = B_0 \cos(\omega t + \psi)
\beta B_0 \cos(\omega t + \psi)
\alpha B_0 \sin(\omega t + \psi)
\gamma = \sqrt{\alpha^2 + \beta^2}
\Delta\psi = -\arctan(-\alpha/\beta)
B_{x,\mathrm{meas}} = \gamma B_0 \cos(\omega t + \psi + \Delta\psi)
\cosh\left(z \over \delta\right)
-\pd{\Phi}{t}

---
Remarks
- gain from thermal shield, eddy current suppresion:
- attenuation parameters:
\beta \sim {1 + e^{-c/\delta} \over 2}
\delta = \sqrt{2 \rho \over \omega \mu_r \mu_0}
\alpha \sim \omega \delta e^{-c/2\delta} \sinh\left(c \over 2\delta\right)
$\lesssim 2 \times 10^{-3}$ deviation from 1